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Epoxidized Soybean Oil Plasticizer CAS 8013-07-8
Epoxidized Soybean Oil Plasticizer CAS 8013-07-8 Properities
[bookmark: _GoBack]Epoxidized Soybean oil (ESO) is a kind of slightly yellow viscous oily liquid,with viscosity of 325mpa.s,refractive index of 1.473 and density of 0.997.Epoxidized soybean oil is not soluble in water,but its soluble in organic solvent,such as hydrocarbon,ketone,lipids,higher alcohols,etc and also slightly soluble in alcohol.
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Epoxidized Soybean Oil Plasticizer CAS 8013-07-8 specifications
	[bookmark: OLE_LINK1]ITEMS
	STANDARD
	RESULT

	EPOXY VALUE (%)
ASTMD1652-04
	6.0MIN
	6.23

	COLOR SHADE(pt-co)
	180MAX
	150

	DENSITY(20℃g/cm3)
	0.988-0.998
	0.9901

	IODINE VALUE (%)
	5.0MAX
	1.74

	ACID VALUE(mg KOH/g)
	0.6MAX
	0.48

	MOISTURE CONTENT(%)
	0.3MAX
	0.03

	FLASH POINT(℃)
	280MIN
	296

	CONCLUSION
	ACCEPT
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