厦门迪太进出口有限公司

XIAMEN DITAI IMP.& EXP. CO.,LTD

地址：中国厦门禾祥西路鸿升大厦8A

8FL, Hongsheng Building, West Hexiang Road, Xiamen, Fujian, China

TEL:0592-26808108 Phone:+8615160094689 FAX:0592-2680880 E-mail: irene.zhang@xmditai.com

----------------------------------------------------------------------------------------------------------------------

Epoxidized Soybean Oil Plasticizer CAS 8013-07-8

Epoxidized Soybean Oil Plasticizer CAS 8013-07-8 Properities

Epoxidized Soybean oil (ESO) is a kind of slightly yellow viscous oily liquid,with viscosity of 325mpa.s,refractive index of 1.473 and density of 0.997.Epoxidized soybean oil is not soluble in water,but its soluble in organic solvent,such as hydrocarbon,ketone,lipids,higher alcohols,etc and also slightly soluble in alcohol.

Epoxidized Soybean Oil Plasticizer CAS 8013-07-8 specifications

| ITEMS | STANDARD | RESULT |
| --- | --- | --- |
| EPOXY VALUE (%) ASTMD1652-04 | 6.0MIN | 6.23 |
| COLOR SHADE(pt-co) | 180MAX | 150 |
| DENSITY(20℃g/cm3) | 0.988-0.998 | 0.9901 |
| IODINE VALUE (%) | 5.0MAX | 1.74 |
| ACID VALUE(mg KOH/g) | 0.6MAX | 0.48 |
| MOISTURE CONTENT(%) | 0.3MAX | 0.03 |
| FLASH POINT(℃) | 280MIN | 296 |
| CONCLUSION | ACCEPT |  |